## Slide 1: Mura - No more mystery
Introduction
Scott Hong
10/07/2019

## Slide 2: Mura : no more mystery
Objective
We can fix the Mura problem ( X )
We narrowed down the root cause of Mura ( Δ )
We can measure the Mura to get quantitative data ( O )
Background
Almost every Echo Show suffered by Mura during development

## Slide 3: Mura : no more mystery
Introduction
Activities is Crown development – Haiwei Chen
pDOT analysis of Mura – Matt Little
Machine leaning algorithm for Mura evaluation – Ahmed Hassan
Mura test fixture – Ming Wang

## Slide 4: Typical Mura symptom

## Slide 5: Typical Mura symptom - realistic
Camera auto exposure
Realistic image to human eyes

## Slide 6: Visible condition of Mura
Mura is not visible when
  the room is bright
  ALS adjust the brightness of backlight in dark environment
  any image other than solid black (+ gray clock) is on
Mura is not a functional defect, but has impact on the reputation

## Slide 7: The origin of the name of “Mura”
Different names are used for our symptom
  Corner Mura
  Stress Mura
  Light leakage
Mura (むら, 斑) : unevenness or stain in Japanese
  Yellow mura, suji mura, COG mura, red eye mura, Corner mura, ...
Mura
Yellow mura
COG mura
Suji mura
Stress mura
Mura
Yellow mura
COG mura
Suji mura
Light leakage

## Slide 8: Yellow Mura vs White (stress) Mura
Yellow Mura : LCD on (white image)
Liquid crystal : bigger optical dispersion (wavelength dependency) makes color change
Cell gap makes the LC thickness changed
White Mura : LCD off (black image)
Glass : smaller optical dispersion makes same polarization rotation across RGB
Cell gap has no relation with white mura in black image
Polarizer
CF glass
TFT glass
Polarizer
Liquid crystal
Column spacers
Cell gap

## Slide 9: The cause or light leakage – polarization rotation in glass
White image
Black image
Light leakage
Polarizer
CF glass
TFT glass
Polarizer
◉ ↔︎
◉
◉ ↔︎
◉ ↔︎
↔ ︎
◉ ↔︎
↔︎
Polarizer
CF glass
TFT glass
Polarizer
◉ ↔︎
◉
◉ ︎
◉ ↔︎
↔︎
◉ ↔︎
↔︎
Polarization rotation
by retardation
Polarizer
CF glass
TFT glass
Polarizer
Liquid crystal
Column spacers
Cell gap
◉ ↔︎
◉
◉
◉
︎
◉
Backlight
S-polarization
P-polarization

## Slide 10: The cause of polarization rotation – glass retardation
Bending induces stress
Stress induces birefringence of glass
No stress
Under stress
ni
ni
ne
no
d
Push
Tensile stress
Glass
Compressive
stress
isotropic
anisotropic

## Slide 11: The cause of glass retardation – Photoelasicity
Photoelasticity
  The changes in the optical properties of a material under mechanical deformation caused by the stress distribution
Setup for polariscope
   Same as LCD stack-up

## Slide 12: The cause of stress – (local) flatness of housing
External housing - curve at corner
Shrinkage of molded part
Result Mura modes

## Slide 13: Bending test - Bishop
L1 = L2 = 30mm
d > 0.4mm
Result
Setup

## Slide 14: Solutions of Mura in display industry
CNC cut from chunk of aluminum
+ $$$$$
Compensation of tools
+ Time
Thinning the LCD glasses
+ $$
In order to make the part flat,
the tool shouldn’t be flat

## Slide 15: Mura : no more mystery
Introduction
Activities is Crown development – Haiwei Chen
pDOT analysis of Mura – Matt Little
Machine leaning algorithm for Mura evaluation – Ahmed Hassan
Mura test fixture – Ming Wang